## Slide 1
SOBHA ACCEPTABLE QUALITY LEVEL (SAQL)
Document Title : | Paint
Document Number : | SCL-SAQL-001
Date of Origin : | 08.05.2026
Date of Revision : | 
Revision Number : | 00
 | PREPARED BY | REVIEWED BY | REVIEWED BY | APPROVED BY | APPROVED BY | APPROVED BY | APPROVED BY
NAME | Mr. Sathishkumar Ravisankar | Mr. Rajeshkumar Lakshmanan | Mr. Thangapandi Rathinam | Mr. Suleyman Celik | Mr. Ayaz Siddiqui | Mr. Senthil Kumar Parasuraman | Mr. Karthikraj Rajendran
SIGNATURE |  |  |  |  |  |  | 
DATE |  |  |  |  |  |  | 

## Slide 2
AMENDMENT SHEET
DATE OF REV | SUBJECT OF THE AMENDMENT | REV. NO.
08/05/2026 | New release | 00

## Slide 3
OBJECTIVES
OBJECTIVE | The objective of this guideline is to provide a standard procedure for Paint Application Acceptable levels according to the Zones.
SCOPE | This document is valid for Paint Application Aesthetics Acceptance.
RESPONSIBLE | Site execution shall strictly adhere to the approved standards. QA/QC and QCS shall use these standards for inspection.
TERMS & REFERENCES | The QM / BE team shall be responsible for revising and updating the applicable standards as required.

## Slide 4
CATEGORIZATION / ZONES
= Ceiling
= Wall
= Corners
= Bulkhead
= Shadow Groove

## Slide 5
DEFECT DESCRIPTION / PARAMETER |  |  | Paint Corner Right Angle |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Right angle scale & Straight Edge | 
 |  |  | STANDING POSITION |  | As required | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | 1mm | 1mm | 1mm | 1mm | 1mm | NA
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Ceiling to Wall
Wall to Wall
Steps :
Place both 3-meter straight edge flush to the corner.
Set the right‑angle square on top, firmly seated at the corner.
Check the corner for squareness, any gap or misalignment
Time of inspection: Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 6
DEFECT DESCRIPTION / PARAMETER |  |  | Paint Undulation |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Straight Edge & Feeler gauge | 
 |  |  | STANDING POSITION |  | As required | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | 1.5 mm every 3 meter (No Waviness) | 1.5 mm every 3 meter (No Waviness) | 1.5 mm every 3 meter (No Waviness) | 1.5 mm every 3 meter (No Waviness) | NA | 1.5 mm every 3 meter (No Waviness)
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Steps :
Place the 3-meter straight edge flat against the surface, ensuring there is no tilt or lifting.
Insert the feeler gauge blade into any visible gap between the straight edge and the surface.
Check the measurement along the entire length.
Time of inspection: Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 7
DEFECT DESCRIPTION / PARAMETER |  |  | Paint Improper Sanding Mark Visibility |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Visual Inspection | 
 |  |  | STANDING POSITION |  | Minimum 1 Meter in any direction. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | NA
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Visual inspection of painted areas shall be carried out under natural daylight or appropriate artificial lighting from all relevant directions.
Time of inspection: Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 8
DEFECT DESCRIPTION / PARAMETER |  |  | Paint Damage |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Visual Inspection | 
 |  |  | STANDING POSITION |  | Minimum 1 Meter in any direction. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | Not Allowed | Not Allowed | Not Allowed | Not Allowed | Not Allowed | Not Allowed
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Visual inspection of painted areas shall be carried out under natural daylight or appropriate artificial lighting from all relevant directions.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 9
DEFECT DESCRIPTION / PARAMETER |  |  | Paint Crack |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Visual Inspection | 
 |  |  | STANDING POSITION |  | Minimum 1 Meter in any direction. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | Not Allowed | Not Allowed | Not Allowed | Not Allowed | Not Allowed | Not Allowed
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Visual inspection of painted areas shall be carried out under natural daylight or appropriate artificial lighting from all relevant directions.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 10
DEFECT DESCRIPTION / PARAMETER |  |  | Paint Touch-Up |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Visual Inspection | 
 |  |  | STANDING POSITION |  | Minimum 1 Meter in any direction. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Visual inspection of painted areas shall be carried out under natural daylight or appropriate artificial lighting from all relevant directions.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 11
DEFECT DESCRIPTION / PARAMETER |  |  | Paint Bubbles |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Visual Inspection | 
 |  |  | STANDING POSITION |  | Minimum 1 Meter in any direction. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Visual inspection of painted areas shall be carried out under natural daylight or appropriate artificial lighting from all relevant directions.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 12
DEFECT DESCRIPTION / PARAMETER |  |  | Improper Paint Finish |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Visual Inspection | 
 |  |  | STANDING POSITION |  | Minimum 1 Meter in any direction. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Visual inspection of painted areas shall be carried out under natural daylight or appropriate artificial lighting from all relevant directions.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 13
DEFECT DESCRIPTION / PARAMETER |  |  | Paint Shade Variation |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Visual Inspection | 
 |  |  | STANDING POSITION |  | Minimum 1 Meter in any direction. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle | Not visible from 1 meter at any angle
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Visual inspection of painted areas shall be carried out under natural daylight or appropriate artificial lighting from all relevant directions.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 14
DEFECT DESCRIPTION / PARAMETER |  |  | Skirting vs Wall paint flushness |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Straight Edge & Feeler gauge | 
 |  |  | STANDING POSITION |  | As required | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | 0.5 mm Max | NA | 0 mm | NA | NA | NA
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Place 3-meter straight edge flat on the skirting against the wall paint surface.
Confirm that the gap measured with a feeler gauge does not exceed 0.5 mm
Time of inspection :Before application of the first coat of paint.
Wall Area
Corner Area
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 15
DEFECT DESCRIPTION / PARAMETER |  |  | Paint - Staircase bottom undulation (Flatness) |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Straight Edge, Feeler gauge | 
 |  |  | STANDING POSITION |  | As required. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | NA | 1mm / Sofit width | NA | NA | NA | NA
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Place the straight edge flat against the painted surface at the staircase bottom.
Ensure the flatness deviation does not exceed 1 mm along the full length.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 16
DEFECT DESCRIPTION / PARAMETER |  |  | Paint - Corner Waviness |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Straight Edge, Feeler gauge | 
 |  |  | STANDING POSITION |  | As required. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | NA | NA | 1 mm | 1 mm (Wall side) 0mm (Metal Side) | 0 mm | NA
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Place the 3‑meter straight edge level flat against the painted wall surface in one direction.
Reposition the 3‑meter straight edge level flat against the wall in the perpendicular direction.
Check and confirm flatness deviation over the full length of the straight edge.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”
Shadow Groove
Wall
Wall

## Slide 17
DEFECT DESCRIPTION / PARAMETER |  |  | Paint – Edge Undulation |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Straight Edge. | 
 |  |  | STANDING POSITION |  | As required. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | NA | NA | 0.5mm for 3 meter | NA | 0 mm | NA
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Place the straight edge level flush against the soffit surface.
Align it fully along the edge, ensuring continuous contact.
Check for gaps to confirm straightness and level.
Time of inspection :Before application of the first coat of paint.
Wall (Internal)Corner Undulation
Ceiling Corner(Exposed corner)
Undulation
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 18
DEFECT DESCRIPTION / PARAMETER |  |  | Paint pattern – Texture vs Smooth (Around MEP Fixtures) |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Visual Inspection | 
 |  |  | STANDING POSITION |  | Minimum 1 Meter in any direction. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | Not Allowed | NA | NA | NA | NA | NA
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Visual inspection of painted areas shall be carried out under natural daylight or appropriate artificial lighting from all relevant directions.
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 19
DEFECT DESCRIPTION / PARAMETER |  |  | Paint - GRG panel line verticality and corner |  |  | 
DEFECT IMAGE / PARAMTER |  |  | MEASURING METHOD |  |  | 
 |  |  | INSTRUMENT / INSPECTION METHOD |  | Putty & Feeler Gauge | 
 |  |  | STANDING POSITION |  | As required. | 
APPLICABILITY |  VILLA  APARTMENT |  | LIGHTING |  | Natural / Ambient light / Artificial Light | 
ACCEPTABLE QUALITY LEVEL |  |  |  |  |  | 
SCENARIO / LOCATION / ZONE | Wall | Ceiling | Corners | Shadow Groove | Bulkhead | Cove Light
ACCEPTANCE LIMIT | NA | 0.5mm for 3mtr | NA | NA | NA | NA
REMARKS |  |  |  |  |  | 
PAINT - SAQL
Place the straight edge flat on the edge against the wall paint surface.
Confirm that the gap measured with a feeler gauge does not exceed 0.5 mm
Time of inspection :Before application of the first coat of paint.
“Note: During keep-out inspection in case of any visual discrepancy identified, measurement verification shall be carried out based on the SAQL.”

## Slide 20
Thank you
In case any details are required, please contact the QM-QAQC@sobha-me.com.